Caledonian Cables

Automotive Cable

EB/HDEB

Application:

This PVC insulated single-core cable is used in low voltage circuits of battery for automobiles.

Construction:

Copper conductor PVC insulation

Conductor: Cu-ETP1 according to JIS C 3102

Insulation: PVC

Standard Compliance: JIS C 3406

Features:

EB wires is for grounding (-side) and thin type; It consists of complex stranded conductors (flexible type).

HDEB wires are thicker type than EB wires to provide increased mechanical strength.

Technical Parameters:

Operating temperature: –40 °C to +100 °C

| EB |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Conductor |  |  | Insulation | Cable |  |  |
| Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Electrical Resistance at 20°C max. | Thickness Wall nom. | Overall Diameter min. | Overall Diameter max. | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | mm | kg/km |
| 1 x5 | 63/0.32 | 3.10 | 3.58 | 0.60 | 4.30 | 4.70 | 57 |
| 1 x9 | 112/0.32 | 4.20 | 2.00 | 0.60 | 5.40 | 5.80 | 95 |
| 1 x15 | 171/0.32 | 5.30 | 1.32 | 0.60 | 6.50 | 6.90 | 147 |
| 1 x20 | 247/0.32 | 6.50 | 0.92 | 0.60 | 7.70 | 8.00 | 207 |
| 1 x30 | 361/0.32 | 7.80 | 0.63 | 0.60 | 9.00 | 9.40 | 303 |
| 1 x40 | 494/0.32 | 9.10 | 0.46 | 0.60 | 10.30 | 10.80 | 374 |
| 1 x50 | 608/0.32 | 10.10 | 0.37 | 0.60 | 11.30 | 11.90 | 473 |

www.caledonian-cables.co.uk	www.addison-cables.com	37

Caledonian Cables

Automotive Cable

| EB |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Conductor |  |  | Insulation | Cable |  |  |
| Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Electrical Resistance at 20°C max. | Thickness Wall nom. | Overall Diameter min. | Overall Diameter max. | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | mm | kg/km |
| 1 x60 | 741/0.32 | 11.10 | 0.31 | 0.60 | 12.30 | 12.90 | 570 |
| HDEB |  |  |  |  |  |  |  |
| 1 x9 | 112/0.32 | 4.20 | 2.00 | 1.00 | 6.20 | 6.50 | 109 |
| 1 x15 | 171/0.32 | 5.30 | 1.32 | 1.10 | 7.50 | 8.00 | 161 |
| 1 x20 | 247/0.32 | 6.50 | 0.92 | 1.10 | 8.70 | 9.30 | 225 |
| 1 x30 | 361/0.32 | 7.80 | 0.63 | 1.40 | 10.60 | 11.30 | 331 |
| 1 x40 | 494/0.32 | 9.10 | 0.46 | 1.40 | 11.90 | 12.60 | 442 |
| 1 x60 | 741/0.32 | 11.10 | 0.31 | 1.60 | 14.30 | 15.10 | 655 |

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

38	www.caledonian-cables.co.uk	www.addison-cables.com