Caledonian Cables

Automotive Cable

FLR13Y-B

Application and Description:

This TPE insulated low-tension automotive cable is used in motorcycles and other motor vehicles for starting ,charging,lighting,signal and instrument panel circuits.

Cable Construction:

Copper conductor TPE-E insulation

Conductor:Cu-ETP1 bare according to DIN EN 13602

Insulation:TPE-E

Standard:

ISO 6722 Class D

Special properties: Limited resistance to hydrolysis Technical Parameters:

Operating temperature: �40癈 to +150癈

|  | Conductor Construction | Insulation | Cable |
| --- | --- | --- | --- |
| Nominal cross- section | No. and Dia. of Wires | Diameter of Conductor max. | Electrical resistance at 20癈 max. | Nominal thickness | Overall Diameter Min. | Overall Diameter Max. | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | mm | kg/km |
| 1x 0.35 | 12/0.21 | 0.9 | 52.0 | 0.20 | 1.2 | 1.4 | 5 |
| 1x 0. 5 | 16/0.21 | 1.0 | 37.1 | 0.22 | 1.4 | 1.6 | 6 |
| 1x 0. 75 | 24/0.21 | 1.2 | 24.7 | 0.24 | 1.7 | 1.9 | 9 |
| 1x1 | 32/0.21 | 1.35 | 18.5 | 0.24 | 1.9 | 2.1 | 12 |
| 1x 1.5 | 30/0.26 | 1.7 | 12.7 | 0.24 | 2.2 | 2.4 | 16 |
| 1x 2 | 30/0.31 | 2.0 | 9.42 | 0.28 | 2.5 | 2.8 | 23 |
| 1x 2.5 | 50/0.26 | 2.2 | 7.6 | 0.28 | 3.7 | 3.0 | 26 |
| 1x4 | 56/0.31 | 2.75 | 4.71 | 0.32 | 3.4 | 3.7 | 41 |
| 1x6 | 84/0.31 | 3.3 | 3.14 | 0.32 | 4.0 | 4.3 | 60 |

Note: Other configurations, sizes, colors and length not specified herein are available upon reques

34	www.caledonian-cables.co.uk	www.addison-cables.com