Caledonian Cables

Automotive Cable

FLRY-A

Application:

This PVC insulated single-core cable with symmetrical conductor structure (type A) and thin wall is used

for automobiles, Motorcycles electrical equipment in high temperature condition.

Construction:

Copper conductor PVC insulation

Conductor: Cu-ETP1 bare or tinned copper according to DIN EN13602

Insulation: PVC

Standard Compliance: ISO 6722 Class B

Technical Parameters:

Operating temperature: –40°C to 105°C

|  | Conductor |  |  | Insulation | Cable |  |
| --- | --- | --- | --- | --- | --- | --- |
| Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Resistance at 20°C Bare/Tinned max. | Thickness Wall min. | Overall Diameter max. | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | kg/km |
| 1x0.22 | 7/0.21 | 0.70 | 84.80/86.50 | 0.20 | 1.20 | 3 |
| 1x0.35 | 7/0.26 | 0.80 | 52.00/54.50 | 0.20 | 1.30 | 5 |
| 1x0.50 | 19/0.19 | 1.00 | 37.10/38.20 | 0.22 | 1.60 | 7 |
| 1x0.75 | 19/0.23 | 1.20 | 24.70/25.40 | 0.24 | 1.90 | 9 |
| 1x1.00 | 19/0.26 | 1.35 | 18.50/19.10 | 0.24 | 2.10 | 11 |
| 1x1.50 | 19/0.32 | 1.70 | 12.70/13.00 | 0.24 | 2.40 | 16 |
| 1x2.00 | 19/0.37 | 2.00 | 9.42/9.69 | 0.24 | 2.60 | 23 |
| 1x2.50 | 19/0.41 | 2.20 | 7.60/7.80 | 0.28 | 3.00 | 26 |

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

14	www.caledonian-cables.co.uk	www.addison-cables.com