Caledonian Cables

Automotive Cable

FLYY

Application:

This PVC insulated single-core unshielded low-tension wire is used for automobiles, Motorcycles and other motor vehicles.

Construction:

Copper conductor PVC insulation PVC sheath

Conductor: Cu-ETP1 bare according to DIN EN 13602

Insulation: PVC

Sheath: PVC

Standard Compliance: ISO 6722

Technical Parameters:

Operating temperature: –40°C to 90°C

|  | Conductor |  |  | Insulation |  | Cable |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Electrical Resistance at 20°C max. | Thickness Wall nom. | Diameter of Core | Sheath Thickness Nom. | Overall Diameter min. | Overall Diameter max. | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | mm | mm | mm | kg/km |
| 1x0.50 | 16/0.21 | 1.00 | 37.10 | 0.60 | 2.10 | 0.40 | 2.70 | 3.10 | 14 |
| 1x0.75 | 24/0.21 | 1.20 | 24.70 | 0.60 | 2.30 | 0.40 | 3.00 | 3.30 | 17 |
| 1x1.00 | 32/0.21 | 1.35 | 18.50 | 0.60 | 2.50 | 0.40 | 3.20 | 3.60 | 20 |
| 1x1.50 | 30/0.26 | 1.70 | 12.70 | 0.60 | 2.80 | 0.50 | 3.70 | 4.10 | 28 |
| 1x2.00 | 40/0.26 | 2.00 | 9.42 | 0.60 | 3.00 | 0.50 | 3.90 | 4.30 | 33 |
| 1x2.50 | 50/0.26 | 2.20 | 7.60 | 0.70 | 3.50 | 0.50 | 4.30 | 4.80 | 41 |

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

12	www.caledonian-cables.co.uk	www.addison-cables.com