Caledonian Cables

Automotive Cable

FLYZ

Application:

This PVC insulated multi-cores cable is used in internal wiring in automobile where high flexibility, thermo and mechanical strength are required.

Construction:

PVC insulation Copper conductor

Conductor:

Cu-ETP1 bare according to DIN EN13602

Insulation: Plasticized (PVC)

Standard Compliance: ISO 6722

Technical Parameters:

Operating temperature: –25 °C to +90 °C

|  | Conductor |  |  | Insulation |  | Cable |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Electrical Resistance at 20°C max. | Thickness Wall nom. | Diameter of Core | Diameter Width | Diameter Height | Weight approx. |
| mm2 | No./mm | mm | mΩ/m | mm | mm | mm | mm | kg/km |
| 2 x0.50 | 16/0.21 | 1.00 | 37.10 | 0.50 | 2.10 | 4.40±0.20 | 2.10±0.15 | 20 |
| 2 x0.75 | 24/0.21 | 1.20 | 24.70 | 0.60 | 2.35 | 4.70±0.30 | 2.35±0.15 | 23 |
| 2 x1.00 | 32/0.20 | 1.50 | 19.50 | 0.60 | 2.55 | 5.10±0.30 | 2.60±0.15 | 32 |
| 2 x1.50 | 48/0.26 | 1.70 | 12.70 | 0.60 | 2.80 | 5.60±0.30 | 2.80±0.15 | 39 |

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

22	www.caledonian-cables.co.uk	www.addison-cables.com