Caledonian Cables

Automotive Cable

GPT

Application:

This PVC insulated single-core cable is used in automotive applications for general circuit wiring and

automotive or marine applications where 105°C is required.

Construction:

Copper conductor PVC insulation

Conductor: Soft-annealed copper according to ASTM B3

Insulation: PVC

Standard Compliance: SAE J1128

Technical Parameters:

Operating temperature: –40 °C to +80 °C

|  | Conductor |  |  | Insulation |  | Cable |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Size | Nominal Cross- section | No. and Dia. of Wires | Diameter max. | Thickness Wall min. | Thickness Wall nom. | Overall Diameter max. | Weight approx. |
| AWG | mm2 | No./mm | mm | mm | mm | mm | kg/km |
| 22* | 1 x 0.35 | 7/0.25 | 0.76 | - | 0.58 | 2.10 | 7 |
| 20 | 1 x 0.50 | 7/0.32 | 0.97 | 0.41 | 0.58 | 2.40 | 10 |
| 18 | 1 x 0.80 | 16/0.25 | 1.17 | 0.41 | 0.58 | 2.50 | 12 |
| 18 | 1 x 0.80 | 19/0.23 | 1.17 | 0.41 | 0.58 | 2.50 | 12 |
| 16 | 1 x 1.00 | 19/0.28 | 1.45 | 0.41 | 0.58 | 2.90 | 17 |
| 14 | 1 x 2.00 | 19/0.36 | 1.80 | 0.41 | 0.58 | 3.20 | 25 |
| 12 | 1x 3.00 | 19/0.45 | 2.29 | 0.46 | 0.66 | 3.80 | 38 |
| 10 | 1 x 5.00 | 19/0.57 | 2.87 | 0.55 | 0.79 | 4.70 | 59 |
| 8** | 1 x 8.00 | 19/0.73 | 3.26 | 0.66 | 0.94 | 6.00 | 96 |

*for Ford ESF M1L56-A Applications only

** For SAE J1128 and UTMS applications only

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

40	www.caledonian-cables.co.uk	www.addison-cables.com