Caledonian Cables

Automotive Cable

HDT

Application:

This PVC insulated single-core cable is used for automobiles, motorcycles and other motor vehicles.

Construction:

Copper conductor PVC insulation

Conductor: Soft-annealed copper according to ASTM B3

Insulation: PVC

Standard Compliance: SAE J1128

Technical Parameters:

Operating temperature: –40 °C to +85 °C

|  | Conductor |  |  | Insulation |  | Cable |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Size | Nominal Cross- section | No. and Dia. of Wires | Diameter max. |  | Thickness Wall nom. | Overall Diameter max. | Weight Approx. |
| AWG | mm2 | no./mm | mm |  | mm | mm | kg/km |
| 20 | 1x0.50 | 7/0.31 | 1.00 |  | 0.91 | 2.80 | 14 |
| 18 | 1x0.80 | 16/0.26 | 1.50 |  | 0.94 | 3.00 | 20 |
| 16 | 1x1.00 | 19/0.29 | 1.50 |  | 1.02 | 3.50 | 25 |
| 14 | 1x2.00 | 19/0.36 | 1.80 |  | 1.04 | 3.90 | 33 |
| 12 | 1x3.00 | 19/0.45 | 2.30 |  | 1.17 | 4.60 | 49 |
| 10 | 1x5.00 | 19/0.57 | 3.00 |  | 1.17 | 5.30 | 71 |
| 8 | 1x8.00 | 49/0.45 | 3.70 |  | 1.40 | 6.50 | 98 |

*Note: Other configurations, sizes, colors and length not specified herein are available upon request.

www.caledonian-cables.co.uk	www.addison-cables.com 71