Caledonian Cables

Automotive Cable

STX

Application and Description:

This XLPE insulated low-tension automotive cable is used in motorcycles and other motor vehicles for starting ,charging,lighting,signal and instrument panel circuits.

Cable Construction:

Copper conductor XLPE insulation

Conductor:Soft-annealed copper according to ASTM B Insulation:XLPE(Polyethylene crosslinked) Standard:

SAE J 1127

Special properties:

Flame retardant

Highly resistant against acids,lyes,petrol and diesel

Technical Parameters:

Operating temperature: –40°C to +125°C

| Conductor Construction |  |  |  | Insulation |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Size | Nominal cross- section | No. and Dia. of Wires | Diameter of Conductor max. | Nominal thickness | Overall Diameter Max. | Weight approx. |
| AWG | mm2 | No./mm | mm | mm | mm | kg/km |
| 6 | 1x13 | 133/0.36 | 4.83 | 1.09 | 7.80 | 147 |
| 4 | 1x19 | 133/0.46 | 6.09 | 1.12 | 9.50 | 230 |
| 2 | 1x32 | 133/0.57 | 7.67 | 1.12 | 11.00 | 341 |
| 1 | 1x40 | 259/0.46 | 8.49 | 1.12 | 12.00 | 421 |
| 1/0 | 1x50 | 1026/0.26 | 9.47 | 1.12 | 13.00 | 508 |
| 2/0 | 1x62 | 1254/0.26 | 10.47 | 1.12 | 14.50 | 613 |
| 3/0 | 1x81 | 1615/0.26 | 11.98 | 1.12 | 17.00 | 778 |
| 4/0 | 1x103 | 2052/0.26 | 13.40 | 1.12 | 18.50 | 978 |

Note: Other configurations, sizes, colors and length not specified herein are available upon request.

www.caledonian-cables.co.uk	www.addison-cables.com 73